- Fabricate Board per latest revision of IPC-6012

Specification Class 2. Acceptability shall be based on latest revision of IPC-A-600 specificaitons  Class 2.

- Dielectric/Prepreg Material: refer to  gsa0f006a8-Impedance Design(New)-gsa0f006a8.rtf

- Backdrill: the stub lengths  less  than  10mils

- Surface Finished: Imersion Gold(ENIG)

- Silkscreen Color:White

- Soldermask Color:Black

- The via-in-pad  used .plated over with copper and surface finish.The via on SMD with epoxy resin.

- Rotate 10 ° for production

- BOW&Twist:<=0.7%

- Board edge fingers are to be :

50 uinches hard Gold over 200 uinches Nickel plated